A Coupled 3D Wear and Fatigue Numerical Procedure: Application to Fretting Problems in Ultra-High Strength Steel Wires

Authors: I. Llavori1,*, A. Zabala1, J. Mendiguren1, X. Gómez1

1 Mechanical and Industrial Manufacturing Department, Mondragon Unibertsitatea, Loramendi 4, 20500 Mondragón, Spain

*Corresponding author: I. Llavori, (illavori@mondragon.edu)

Abstract:

This work presents a coupled 3D wear and fatigue numerical procedure for fretting problems in ultra-high strength steel wires that combines Archard’s wear equation with the Smith–Watson–Topper parameter to predict crack nucleation. For total life prediction, a mode I crack propagation based on the weight function method was used. To assess fretting fatigue lifetime, several experimental campaigns were run. The numerical results were in good agreement with the fretting fatigue experimental results. Thus, this study provides a 3D numerical methodology to study the combined effects of wear and fatigue in fretting with a case study in ultra-high strength steel wires.

Keywords: Fretting fatigue, fretting wear, wear simulation, multiaxial fatigue, finite element method

Nomenclature

Abreviations

CoF:	coefficient of friction

CoW: coefficient of wear

FIP: 	fatigue indicator parameter

SWT: Smith-Watson-Topper

Symbols

b:	fatigue strength exponent

C:	Paris law coefficient

c:	fatigue ductility exponent

E:	elastic modulus

:	dissipated energy

K:	dimensionless wear coefficient

:	local wear coefficient

:	Fatemi-Socie’s material dependent factor

L:	critical distance

l:	length

M:	Miner’s total accumulated damage

m:	Paris law exponent

Ni:	cycles to crack initiation

P:	contact force

:	contact pressure

Q:	tangential force

R:	stress ratio

s:  	Sliding distance

U:	translational degree of freedom

UR:	rotational degree of freedom

:	wear volume

:	energy wear coefficient

:	scaling down factor

:	applied displacement at the contact point

:	incremental wear depth

:	relative slip

:	stress intensity factor range

:	crack propagation threshold

: 	normal strain amplitude

:	applied displacement

:	fatigue ductility coefficient

:	fatigue strength

:	stress amplitude

: 	fully reversed stress amplitude

: bulk stress

:	maximum stress

: maximum normal stress

:	fatigue strength coefficient

:	yield strength

- Introduction

Wear and fatigue are classical issues encountered in mechanical components and assemblies such as gears, bearings, ropes, overhead conductors and bolted or press-fitted connections. Frequently the two phenomena are linked, and study of them is complex, as such study usually involves, simultaneously, multiaxial non-proportional stresses, high stress gradients and tribological problems. Fretting is a phenomenon that follows the aforementioned failure modes. It is defined as the small oscillatory movement between two or more bodies in contact, usually displacements below 300 µm [1]. Depending on the predominant failure mode – that is, wear-assisted or fatigue-assisted rupture – fretting is divided into fretting wear or fretting fatigue problems, respectively [2].

In recent years fretting research into the failure of ropes and cables has been a very active topic in the literature of the field. As shown in Fig. 1a, ropes are built with many multi-layered strands of thin steel wire. In service, the rope endures high bending loads, which promote movement between the internal wires accelerating their rupture due to fretting phenomena [3]. In Fig. 1b a typical fretting failure of a wire used in the elevator industry is shown. As can be observed, the wire endured both wear and fatigue, indicating that in this case fretting wear and fretting fatigue phenomena are linked.

Wear scar

Fractured surface

Edge of contact

(a)					(b)

Fig. 1. (a) 3D schematic of the construction of a wire rope [3], (b) SEM micrograph showing the fracture of a wire at the edge of the wear scar produced by a combined fretting wear and fretting fatigue problem [4]. Reproduced with permission of Springer.

From the experimental point of view, several test machines have been specifically developed for rope studies [5]. These include machines that analyse the global mechanical response of the whole rope, such as through tension-tension fatigue tests [6], bending fatigue tests [7] and other tests [8], [9]. Other machines have also been developed to study in detail the fretting failure of two contacting wires. These devices can be divided into fretting wear [10], [11] and fretting fatigue testing machines [4], [12]–[14].

In research to understand and predict fretting wear and fretting fatigue failure, numerical models have emerged as useful complements to experimental studies. Therefore, efforts have been made to develop state-of-the-art numerical tools to study the aforementioned failure modes.

Recently, Araújo et al. [15] and Rocha et al. [16] analysed the fretting behaviour of the steel wires used in overhead conductors (4-mm diameter). These conductors are usually subjected to Aeolian vibrations, which promotes fretting problems between the contacting wires. In their 3D numerical model, these researchers neglected wear phenomena, as these conductors primarily work in partial slip conditions. Their model coupled the Smith–Watson–Topper (SWT) fatigue indicator parameter (FIP) with a volume averaging approach to account for the stress gradient effect.

Said et al. [17], [18] also analysed the fretting behaviour of overhead conductors, particularly those made of aluminium with diameters of 2–7 mm. They presented a global–local methodology with the entire strand considered in the global model and a single crossed cylinder contact simulated in the local model. As in the Araujo et al. and Rocha et al. studies, wear phenomena were also neglected in this study. The researchers coupled the Crossland criterion with a crack propagation methodology for fatigue life prediction.

Unlike in the aforementioned studies, wear phenomena cannot be neglected in elevator ropes. The minute movement caused when the rope runs over a sheave promotes a combined fretting wear and fretting fatigue failure, as shown earlier in Fig. 1b. Our previous work employed a crossed cylinder contact configuration (90°) to study the combined effects of fretting wear and fretting fatigue in ultra-high strength steel (UHSS) wires [19]. The numerical modelling considered Archard’s wear equation for wear simulation combined with the SWT FIP for fatigue life prediction. One of the main drawbacks of our work was that the fatigue properties of the UHSS wires studied were not available. In the absence of these fatigue coefficients, the work used data reported by Beretta and Matteazzi [20]. The main drawback of these fatigue constants was that the diameter of the wire Beretta and Matteazzi used was significantly larger than that of the UHSS wires used in our work (1.97 mm vs. 0.45 mm), and different authors have reported that the diameter of the wires has a significant impact on fatigue life [20]–[22]. Therefore, we concluded that a proper experimental campaign testing plain fatigue and fretting fatigue with UHSS wires was of great interest.

This work presents a substantially improved numerical procedure of coupled 3D wear and fatigue for fretting problems in UHSS wires. The model includes a new damage interpolation scheme and considers the stress gradient effect and the compliance of the contact system. In addition, an analytical crack propagation analysis for total life prediction is included to overcome the increase in computational time due to the 3D structure. To validate the model, fretting fatigue, plain fatigue, wear, and friction on UHSS wires have been characterized.

2. Background

This section summarizes the literature reviewed for the research presented in this work. First, an overview of various wear simulation approaches is provided and certain details of our implementation are presented. The reader is referred to previous works for more information regarding implementations of the wear code [23]–[25]. Then, a summary of the multiaxial fatigue assessment and crack propagation analysis is given followed by presentation of this work’s proposal.

2.1. Wear simulation

Wear simulation has been extensively studied over the last two decades. Usually, papers reporting on wear simulation use Simulia Abaqus as their finite element code of choice. This is primarily because the user subroutine UMESHMOTION is readily available to implement any wear equation, and there are several ways to implement such equations [23], [26]–[30].  Typically, Archard’s wear equation and the dissipated friction energy equation are used (eq. 1 and eq. 2):

,							(1)

,						(2)

where is the wear volume,  K is the dimensionless wear coefficient of the material, P is the contact force, s  is the sliding distance, α is the energy wear coefficient, and   is the accumulated dissipated energy. Following the trend, this work uses Archard’s wear equation [23], [31]. In a finite element code, eq.1 is implemented using the modified local equation combined with the cycle jump technique, defined as follows:

,					(3)

where  is the incremental wear depth at a specific point x (node) and time,  is the cycle jump value,  is the local wear coefficient,  and  are the contact pressure and the relative slip, respectively, at a specific point x (node) and time. Additionally, in this study, unlike in previous works, a variable local wear coefficient was considered [19], [23], [24].

2.2. Multiaxial Fatigue Indicator Parameter

Multiaxial FIPs can be classified into three types: strain-based, generally for low-cycle fatigue (LCF); stress-based FIPs for high-cycle fatigue (HCF); and energy-based models, which generally are applicable to both LCF and HCF regimes [32]–[34]. Additionally, FIPs can be divided into critical plane criteria and effective stress-based criteria. Usually, effective stress criteria are not suitable to use with non-proportional stressing, and the critical plane FIPs are recommended for these cases, although effective stress FIPs such as the Crossland criterion have been successfully used for fretting [35], [36]. In this work, the multiaxial SWT FIP within the critical plane approach was evaluated [37]. The SWT parameter is defined as the product of maximum normal stress () and normal strain amplitude ():

,				(4)

where  is the fatigue strength coefficient,  is the fatigue exponent, E is the elastic modulus,  is the fatigue ductility coefficient, c is the fatigue ductility exponent, and is the number of cycles to crack nucleation. Identifying the critical plane in 3D requires a more complex stress and strain transformation and calculation than is required in 2D (the transformation equations used are described in Appendix 1, eqs. 11—25).

In the gross slip regime, the wear phenomenon has a beneficial effect on the fretting fatigue lifetime. This is because the damaged material is removed by wear, which increases the contact area and thus reduces the contact stresses [38]. Therefore, a damage accumulation framework such as the Miner-Palmgren rule (M) [39] is needed to account for the changing stress field with the continuation of cycles:

,						(6)

where  is the estimated number of cycles to initiation by the FIP over the ith fretting cycle.

As described in the previous section, a wear simulation is usually performed by adjusting the nodal coordinates, by means of a wear equation, so that from cycle to cycle the position of a node changes. This means that the accumulated damage of preceding cycles would not be the same for the new coordinates. Because the damage decreases below the surface due to the stress gradient, the accumulated damage at the new coordinates should be smaller. To account for these changes, an interpolation scheme is usually employed. Two different schemes were found in the literature to tackle this problem — (i) the material point mesh (MPM) method, proposed by Madge et al. [40], and (ii) the centroidal damage mesh method (termed CDMM in this work) proposed by Cruzado et al. [19]. In the MPM method, fixed grid points are first defined, and the damage from the ith fretting cycle is linearly interpolated back to the MPM points. In the CDMM the accumulated damage in the ith fretting cycle is linearly interpolated to the current centroidal location. Each method has its own strengths and weaknesses. For example, for large amounts of wear, the latter method is more efficient. However, with the CDMM the accumulated damage is continuously interpolated to the current cycle, so that a small error is accumulated from cycle to cycle. By contrast, in the MPM method the damage from the ith fretting cycle is only once interpolated back to the reference point, so that a smaller error is achieved.  In this study, a new interpolation scheme, coined as the current centroidal point mesh (CCPM) method is presented which is a hybrid approach between the CDMM and the MPM method. In the CCPM method, a complete interpolation of all previous cycles from the original location to the current location is performed, so that the damage of each cycle is always interpolated from the original position (see Fig. 2).

Another important aspect in fretting cases is consideration of the stress gradient effect. Multiple non-local approaches to tackle the stress gradient effect can be found in the literature [16], [41]–[44]. This work employs the volume method of the theory of critical distances using a sphere region, centred in each element centroid, with a radius equal to  [41]:

,						(7)

where is the crack propagation threshold, and is the fatigue strength range.

a)

b)

c)

d)

e)

f)

g)

h)

Fig. 2. Scheme of the developed current centroidal point mesh (CCPM) method for damage accumulation purposes coupled with wear simulation: (a) accumulated damage at the  cycle, (b) incremental damage at the  cycle, (c) incremental damage at the  cycle, (d) accumulated damage at the  cycle interpolated to the  cycle centroidal location, (e) accumulated damage at the  cycle, (f) accumulated damage at the  cycle interpolated to the  cycle centroidal location, (g) accumulated damage at the  cycle interpolated to the  cycle centroidal location, (h) accumulated damage at the  cycle.

2.3. Crack propagation

Crack propagation in combination with wear is a challenging phenomenon to model. Usually a competition takes place between wear and crack growth, in which wear has the potential to remove the crack or reduce its growth rate. Various approaches to numerically studying the crack propagation stage can be found in the literature [9], [45]–[48]. A previous work presented a 2D coupled crack propagation and wear numerical procedure [25]. The numerical architecture developed allowed for the study, in great detail, of the interaction between the two phenomena, although the numerical implementation was complex. One of the main conclusions of that work was that the computational time required to study both phenomena in 3D might be prohibitive, and a simpler approach might be needed. As a first approach, and considering that in experiments the crack is usually straight, a simple mode I stress intensity factor was calculated using the weight function of circular-fronted cracks in cylindrical bars presented by Caspers and Mattheck [49]:

,					(8)

where  is the weight function, and is the crack opening stress range distribution along the prospective crack faces. Once the stress intensity factor is derived, the incremental crack growth is calculated as

. 					(9)

3. Numerical architecture

Combining wear simulation and fatigue analysis in the same simulation is a cumbersome task, as the damage generally decreases with increasing cycles due to wear, as commented in the previous section. Therefore, it is not known a priori how many cycles must be simulated. This work implemented an approach similar to that used in previous work in 2D [25]: namely, the number of cycles to be simulated is not known at the beginning of the numerical analysis but is only defined at the simulation’s end when the accumulated damage reaches a value of 1.

Fig. 3 shows the developed numerical architecture for combined fretting wear and fretting fatigue 3D calculation in a finite element code. Note that wear and fatigue calculations are sequentially coupled. First wear simulation is performed within the Abaqus FEA software through the user subroutine UMESHMOTION, as previously explained in Section 2.1. After the simulation of the cycle is finished, a post-process is performed to calculate the damage. First, a critical plane calculation is defined to determine the values of the parameters of interest: that is, ,, and , among others. Then, the selected FIP (SWT) is calculated and is followed by the volume averaging technique to account for the stress gradient effect. Due to wear, the centroid of the elements changes slightly from cycle to cycle. Therefore, to sum the accumulated damage from previous cycles, the new interpolation scheme CCPM was used.. This process is repeated until the total damage reaches the value of a unit. Once the crack initiation condition is reached, a weight function-based crack propagation analysis is carried out.

Write *.inp and manage folders

FE simulation:

3D Wear subroutine through UMESHMOTION

Damage > 1

START simulation

No

Yes

Critical plane calculation

FIP calculation

Compute Damage of the simulated set of cycles

Interpolation of the previous accumulated Damage to the new centroid location

Compute the new Damage values

Crack propagation

Weight function

Simulation FINISHED

Fig. 3. Flow chart computational sequence for numerical analysis.

4. Application to combined fretting wear and fretting fatigue in thin steel wires

4.1. Experimental tests of combined fretting wear and fretting fatigue

An in-house-built fretting fatigue machine was employed in this work; a detailed description of the tribotester can be found in [4]. This modular machine can perform either fretting wear or fretting fatigue tests, depending on the selected configuration. In the fretting fatigue configuration, the cyclic bulk stress () is applied through a DC motor connected to a mechanical system. This mechanical system can generate an accurate cyclic displacement which is sufficient to apply the desired stress amplitude ( ), calculated as

,						(10)

where is the applied displacement, and is the total length of the wire. At the other end of the wire, the mean stress  is applied (see Fig. 4b) through a screw-type mechanical assembly. The contact force is also applied through a screw system, which is connected to a compression spring to absorb any contact shock loading. Additionally, the contact module can adjust the crossing angle between the wires as shown in Fig. 4a. Note that the entire contact module is attached to a precision linear stage to ensure a precise contact position. Finally, given the straining of the fatigued wire, the fretting displacement is controlled by scaling down the displacement where the is applied:

,							(11)

where is the applied displacement amplitude at the contact point, and  is the scaling down factor.

Contact point

Crossing angle

σa

P

P

Multi-axis sensors

σm

Fig. 4. A detailed view of the self-made tribotester with the main parameters shown.

An experimental test program was carried out to compare fretting fatigue lifetime predictions. The test conditions were selected to reflect the real rope contact, displacement amplitude and stress amplitude values [50]. The selected mean stresses, however, were greater than those in working conditions due to the high computational demand required for wear simulation.  Under real rope service conditions, the internal wire breakage usually happens after a large number of cycles (>106 cycles), which is too computationally expensive for 3D wear simulation. Nevertheless, the overall stress field was kept below the yielding strength of the wire. Finally, Table 1, Table 2 and Table 3 summarise the test program, employed test conditions and material properties, respectively.

Table 1. Fretting fatigue test program.

| Test | Mean Stress (σm) | Stress Amp. (σa) | Contact Load (P) | Stroke (2Δ) | Crossing Angle |
| --- | --- | --- | --- | --- | --- |
| - | MPa | MPa | N | µm | ° |
| 1–2 | 1500 | 270 | 3 | 100 | 90 |
| 3–4 | 1250 | 270 | 3 | 100 | 90 |
| 5–6 | 1250 | 270 | 3 | 150 | 90 |
| 7–8 | 1500 | 270 | 3 | 100 | 60 |
| 9–10 | 1500 | 270 | 3 | 100 | 30 |
| 11–12 | 1250 | 270 | 3 | 100 | 60 |
| 13–14 | 1250 | 270 | 3 | 100 | 30 |

Table 2. Fretting tribological test conditions.

| Properties | Symbol | Unit | Value | Tribosystem |
| --- | --- | --- | --- | --- |
| Tangential stress ratio | RQ | - | -1 | P P 2Δ* |
| Frequency | υ | Hz | 5 |  |
| Lubricant |  | - | None |  |
| Temperature | T | °C | 22±2 |  |
| Atmosphere |  | - | Laboratory air |  |
| Relative humidity | RH | % | 50±5 |  |

Table 3. Geometrical, mechanical and surface properties of cold drawn eutectoid carbon steel (0.8% C).

| Properties | Symbol | Unit | Value |
| --- | --- | --- | --- |
| Fatigued wire length | lwire | mm | 155 |
| Wire diameter | d | mm | 0.45 |
| Tensile strength | σu | MPa | >3200 |
| Yield strength | σy | MPa | >2650 |
| Elastic modulus | E | GPa | 205 |
| Vickers hardness | HV0.05 | - | 659±81 |
| Average roughness drawn direction (DD) | Ra | μm | 0.35 |
| Average roughness perpendicular to the DD | Ra | μm | 0.7 |

4.2 Friction and wear coefficients calibration tests

In previous works both the friction and wear coefficients were calibrated with the same steel wire used in this work (see Fig. 5). Detailed analyses and the methods used to characterize both coefficients can be found in [10], [50]. Finally, Table 4 summarises the calibrated values of friction and wear coefficients determined in the present work.

- (b)

Fig. 5. Friction and wear test results: (a) evolution of the coefficient of friction  [50], (b) the total wear volume with respect to Archard’s loading factor for a stroke of 65 µm [10]. Reproduced and adapted with permission of Elsevier.

Table 4. Summary of the calibrated coefficient of wear (CoW) and friction  (CoF).

| Wire | CoW (Running-in) | CoW (Stable Period) | CoF |
| --- | --- | --- | --- |
| Contact wire |  |  | 0.62 |
| Fatigued wire |  |  | 0.62 |

4.3 Material fatigue constants calibration tests

Basquin parameters — that is, the fatigue strength coefficient  and fatigue strength exponent b — were obtained from fatigue tests carried out in the elastic regime (see Table 5 and Fig. 6). Due to the buckling effect, it was not possible to test at R = -1. To correct the mean stress effect and thus obtain the Basquin parameters in fully reversed tension-compression tests, the Goodman mean stress correction equation was used:

,							(10)

where  is the fully reversed stress amplitude.

Table 5. Plain fatigue test program results

| Test | Mean Stress | Stress Amplitude | Failure |
| --- | --- | --- | --- |
| - | MPa | MPa | Cycles |
| 1 | 1,220 | 487 | 1,026,422 |
| 2 | 1,276 | 1,224 | 4,998 |
| 3 | 1,327 | 1,273 | 3,247 |
| 4 | 1,374 | 1,326 | 2,489 |
| 5 | 1,425 | 1,375 | 1,753 |
| 6 | 732 | 477 | 23,845 |
| 7 | 720 | 497 | 20,803 |
| 8 | 717 | 496 | 18,269 |
| 9 | 634 | 358 | 78,595 |
| 10 | 633 | 356 | 56,293 |
| 11 | 623 | 366 | 461,073 |
| 12 | 554 | 301 | 493,069 |
| 13 | 565 | 300 | 284,498 |
| 14 | 541 | 292 | 116,165 |
| 15 | 773 | 452 | 43,107 |
| 16 | 768 | 452 | 22,324 |
| 17 | 766 | 451 | 40,578 |
| 18 | 1,475 | 280 | 160,550 |

Fig. 6. Fatigue experimental test results with Basquin fit.

Coffin–Manson parameters — that is, the fatigue ductility coefficient and fatigue ductility exponent c — were estimated using the medians method introduced by Meggiolaro and Castro [51]. This method combines an acceptable average life estimation with one of the lowest standard deviations among similar methods [52]. Finally, the crack propagation threshold value and Paris coefficients were taken from Lambrighs et al. [53], [54]. Table 6 presents the calibrated parameters employed in the SWT FIP for fatigue life prediction.

Table 6. Summary of calibrated parameters for fatigue life prediction. The crack propagation threshold and Paris constants were taken from [53], [54]

|  | b |  | c |  |  | C | m | L |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| MPa | - | - | - | MPa | MPa m1/2 | m/cycle/ (MPa m1/2)m | - | µm |
| 11865 | -0.2558 | 0.45 | -0.59 | 486 | 3.9 |  | 5.44 | 31 |

4.4 Finite element modelling

A Python script was developed to generate automatically the numerical model under different contact and loading conditions. Fig. 7 shows the element geometry used in the numerical model. An eight-node brick-type element was used with further refinement in the contact area to (i) define an accurate stress field distribution and (ii) perform a detailed wear simulation (five layers of elements were considered for wear simulation).

5 Layers

Contact partition zone

5 Layers

U1

U2

U3

U1

U2

U3

U1

U2

UR3

U3

U2

UR1

Fig. 7. Finite element model with detail of the contact partition zone shown, highlighting the number of element layers in which the wear simulation is performed.

Fig. 8 shows the boundary conditions and applied load employed. Given the symmetry in the bulk load axis, only one contact was simulated. A contact force P was applied to a reference node which was connected to the upper part of the contacting wire through a kinematic coupling. Additionally, a spring was introduced to simulate the contact system stiffness. This factor was key to replicating the fretting loop observed in the experiments in our previous work [55]. The cyclic axial bulk load was applied at the right end of the wire while a displacement boundary condition was introduced at the left end, so that at the contact point the actual displacement amplitude was equal to the displacement when the tangential load Q crosses the origin (0).

Coupling

U1, U3, UR1, UR2, UR3 = 0

U1, UR1, UR2, UR3 = 0

U2 = 0

P

U1

U2

UR3

Fig. 8. Finite element loading and boundary conditions.

Fig. 9 shows the fretting cycle history, which was divided into three simulation steps. In the first step, a contact load P was applied to the upper specimen (time increments from zero to one). In the second step, the mean stress was applied to the right end of the lower wire (time increments from one to two). Additionally, to keep the contact point centred, a displacement equal to the straining of the wire from the applied mean stress was introduced at the left end of the specimen (see Fig. 9b). Lastly, a cyclic displacement and the stress amplitude were applied in unison (time increments from two to three). The last step was repeated to track the evolution of the damage in combination with wear.

(a)							(b)

Fig. 9. Finite element steps: (a) normal and bulk stress, (b) applied displacement.

5. Results and discussion

5.1 Numerical model validation: Contact and slip analysis

The numerical model was validated using a theoretical-experimental comparison. On the one hand, the contact pressure was compared with the Hertzian theory:

,					(11)

where r is the radial coordinate defined from the centre of the circular contact, pmax is the maximum contact pressure, and a is the contact radius. Fig. 10 shows the contact pressure distribution for different element sizes for an unworn crossed cylinder case. It can be observed that for the greatest element size, the accuracy is reduced (10 µm). However, as the size of the elements decreases, the convergence of the numerical model is achieved. It should be noted the contact area increases rapidly in the first hundred cycles due to wear, so the initial element size is not crucial in the gross slip regime. In view of these results, an element size of 10 µm was selected as a trade-off between accuracy and computational efficiency.

Fig. 10. Contact pressure distribution comparison calculated by finite element method with Hertzian theory for different element sizes.

An additional important validation in fretting cases is the tangential stress along the contact. In the gross slip regime, the shear stress is proportional to the contact pressure according to the Amontons–Coulomb friction law. This analysis therefore will not give additional information beyond what is described in Fig. 10, as the shear stress is proportional to the contact pressure. However, an experimental comparison of the evolution of the tangential load and slip amplitude could reveal the contact mechanics behaviour during the wear process. Fig. 11 shows a numerical–experimental comparison of the evolution of the fretting loop during the wear process at two different stages. It can be seen that the numerical model follows the same trend that was observed in the experimental simulation. Due to wear, non-Coulomb behaviour (increase of the tangential load at the end of the stroke) was observed in both the experimental and numerical simulations, as was a decrease of the slip amplitude.  Therefore, it was concluded that the developed numerical model replicates with accuracy the key variables in fretting, and it can be used to analyse the interaction between wear and fatigue.

Fig. 11. Experimental and numerical correlation of the evolution of the fretting loop for different numbers of cycles.

5.2 Crack initiation location

To predict the crack initiation location, three representative tests with different crossing angles were selected (90°, 60°, and 30° crossing angles). As shown in the literature [56], the wear track shape is dependent on the crossing angle between the contacting wires, and thus the crack location might change when the crossing angle is changed. Fig. 12 shows the experimental correlation of the estimated crack locations for Test 5 (90°, left column) and Test 7 (60°, right column). In the case of Test 5, the numerical analysis predicts the crack initiation at the trailing edge of the contact, at exactly the same location seen in the experimental test (see Fig. 12a, b and c). The subsequent crack propagation is almost straight until the final stage of crack growth, when it deviates towards the centre of the wear track located on the second fretting contact (see Fig. 12d).  As shown by Gonzalez et al. [57], this behaviour is attributed to the strongly aligned microstructure due to the wire drawing process.

The right column of Fig. 12 shows the numerical and experimental comparison for Test 7 (90° crossing angle). It can be seen that the numerical model predicts two crack locations near the leading and trailing edges of the contact (see Fig. 12e and f). The experimental test shows the same trends, with two cracks at the locations predicted by the numerical model (Fig. 12g). In this case, the crack located at the leading edge was the one that propagated until the final fracture. Similar to the previously analysed Test 5, the crack deviated during the final stage, in this case toward the trailing edge of the other fretting contact (see Fig. 12h).

Crack

Wear track prediction

Damage box

Crack prediction

Wear track shape

Fracture surface

Contact Side 1

Contact Side 2

Contact Side 1

Wear track shape

Crack

Crack prediction

Damage box

Contact Side 2

Crack

Wear track

Fracture surface

Wear track prediction

Wear track shape

a

b

c

d

e

f

g

h

Test 5

Test 7

Fig. 12. Experimental and numerical correlation of crack location for Test 5 (a–d) and Test 7 (e–h) tests: (a) crack nucleation prediction, (b) wear track prediction, (c) experimental location of the crack of one of the contact sides, (d) experimental location of the final fracture on the other fretting contact side, (e) crack nucleation prediction, (f) wear track prediction, (g) experimental location of the crack of one of the contact sides, (h) experimental location of the final fracture on the other fretting contact side.

Fig. 13 shows the obtained results for the Test 9 (30° crossing angle). The crack initiation location is similar to Test 7 (Fig. 12e), however a more extended damaged area can be observed (see Fig. 13a). On the other hand, Fig. 13c shows that the fatigued wire fractured outside the fretting contact. This was also the result in Test 10, which was a repetition of Test 9.  One possible explanation for this behaviour is that the generated crack was not able to propagate, and a defect outside the fretting contact may have been the weakest link.

Wear track prediction

Damage box

Crack prediction

a

b

c

Fig. 13. Experimental and numerical correlations of crack location for Test 9-10: (a) crack nucleation prediction, (b) wear track prediction, (c) experimental location of the crack outside of the fretting contact.

5.3 Lifetime assessment

Table 7 and Fig. 14 compare the predicted numbers of cycles until crack initiation and crack propagation to the experimental counterparts. From these results, it can be concluded that the lifetime predictions by the proposed numerical procedure fall within the usual scatter band. It should be mentioned that for the tests with a crossing angle of 30°, the numerical model predicted failure within the fretting contact. In experiments for Tests 9 and 10, however, the fracture of the wires happened outside the contact. As previously discussed, this may have been because once the crack was generated, its growth could be relatively slow compared to a defect outside the contact.

Table 7. Comparison between predicted lifetime and experimental results. Error is presented as a percentage change with respect to the experimental lives. Note: * fracture outside the fretting contact zone. ** No fracture.

| Test | Experimental Life | Crack Initiation Prediction | Crack Propagation Prediction | Total Life | Error |
| --- | --- | --- | --- | --- | --- |
| - | Cycles | Cycles | Cycles | Cycles | % |
| 1-2 | 24,619-26,568 | 20,668 | 7,305 | 27,973 | 5.28-13.62 |
| 3-4 | 96,051-104,689 | 33,062 | 76,233 | 109,295 | 4.39-13.78 |
| 5-6 | 34,547-40,599 | 25,305 | 7,173 | 32,478 | -20.0- -5.98 |
| 7-8 | 16,234-18,597 | 28,449 | 10,748 | 39,197 | 110.77-141.45 |
| 9-10 | 135,754*-156,184* | 34,496 | 15,428 | 49,924 | -67.99- -63.22 |
| 11-12 | 172,541-204,789 | 41,825 | 84,997 | 126,822 | -38.07- -26.49 |
| 13-14 | 500,000** | 64,214 | 128,543 | 172,757 | - |

Error factor of 3

Fig. 14. Correlation between predicted and experimental lives.

Fig. 15 shows the percentages of the predicted lives under crack initiation and crack propagation stages. It can be observed that the percentage is heavily influenced by the mean stress. Higher mean stress (MPa, Test 1-2, 5-6, 7-8, and 9-10) tends to result in a larger percentage of lifetime in the crack nucleation stage. By contrast, lower mean stress (MPa,10 Test 3-4, 11-12, and 13-14) tends to result in a longer propagation stage representing approximately 75% of the total number of cycles to failure.

Fig. 15. Predicted percentage of combined fretting wear and fretting fatigue crack nucleation and propagation lifetime:  MPa (Test 1-2, 5-6, 7-8, 9-10) and   MPa  (Test 3-4, 11-12, 13-14).

The influences of slip amplitude and crossing angle on the different test groups were also analysed. For Tests 1-2 and Tests 6-7, the strokes were changed, to 100 µm and 150 µm, respectively, while all the other parameters were kept the same (see Table 1). Both experimental and numerical models predicted a greater number of cycles to failure for larger slip amplitudes. This is because larger slip amplitudes generate larger and deeper wear tracks (see Fig. 16) and thus lower contact stresses.

336 µm

288 µm

a

b

Fig. 16. Comparison of the wear track shapes with different slip amplitudes: a) Test 1-2  2Δ = 100 µm; b) Test 6-7,  2Δ = 150 µm.

Two groups were selected for an analysis of the effect of the crossing angle: Group 1) Test 3-4 (90°), Test 11-12 (60°), and Test 13-14 (30°) and Group 2) Test 1-2 (90°), Test 7-8 (60°), and Test 11-12 (30°). Similar to the slip amplitude analysis, in each group all other parameters were kept the same (see Table 1 for more detail).  In the first group, the experimental test showed higher numbers of cycles to failure for smaller crossing angles. This is because smaller crossing angles tend to generate lower contact pressures, and thus longer fretting lives are expected. It can be observed that the  numerical model predicted the same tendencies. It should be noted that in the second test group the test with a crossing angle of 60° showed shorter lives than the test with a 90° angle, an outcome not predicted by the numerical model. The differences, however, are within the usual scatter band. Therefore, it was concluded that the numerical model shows the same general trends as the experimental tests and is a powerful tool with robust predictive capabilities.

6. Conclusions

This study analysed the viability of combined wear and fatigue numerical procedures for fretting fatigue lifetime estimation in ultra-high strength steels. For total life prediction, as a first approach a simple mode based on the weight function method was used to estimate the crack propagation number of cycles. To validate the proposed model, an in-house-built test rig was used, and plain fatigue, friction and wear coefficients were calibrated. Based on these results, the following conclusions may be drawn:

- Accurate overall lifetime predictions were obtained. Therefore, a reliable and robust 3D numerical approach is presented to predict fretting fatigue lifetime. The Basquin coefficients calibration of the UHSS wires was a key step in obtaining a reliable tool, as our previous work had suggested.

- Crack initiation locations were predicted accurately for various cases, and it was determined that the crack location is dependent on the crossing angle.

- The lifetime percentages under crack initiation and crack propagation might be dependent on the mean stress. The numerical model predicted longer crack initiation stages for higher mean stresses.

- Larger slip amplitudes tend to increase fretting fatigue lifespan, as the removal of material tends to decrease the contact stresses.

- Generally, higher crossing angles result in shorter fretting fatigue lifetimes.

- The implementation of the contact system stiffness in the numerical model was a key factor in replicating the contact behaviour during wear process, allowing an accurate multiaxial analysis.

- A novel damage interpolation scheme, coined as CCPM, is proposed in which the damage of each cycle is always interpolated from the original position, minimizing errors.

Acknowledgments

The authors gratefully acknowledge the financial support given by Orona EIC and the Eusko Jaurlaritza under “Programa de apoyo a la investigación colaborativa en áreas estratégicas” (Project MEDECA: Ref. KK-2017/00053, and MEDECA2: Ref. KK-2018/00013) programs.

Appendix A

This appendix describes the transformation equations employed to define the stresses and strains at any given plane [58]. The equations of normal and shear stresses in a plane is given by the following expressions:

(11)

(12)

(13)

Where the terms are:

(14)

(15)

(16)

(17)

(18)

(19)

(20)

(21)

(22)

The strain equations,, and  are analogous to ,, and  , however, only half of the shear strains needs to take into account:

(23)

(24)

(25)

References

[1]	O. Vingsbo and S. Soderberg, “On Fretting Maps,” Wear, vol. 126, pp. 131–147, 1988.

[2]	R. B. Waterhouse, “Fretting Wear,” Wear, vol. 100, pp. 107–118, 1984.

[3]	M. A. Urchegui, W. Tato, and X. Gómez, “Wear evolution in a stranded rope subjected to cyclic bending,” J. Mater. Eng. Perform., vol. 17, no. 4, pp. 550–560, 2008.

[4]	I. Llavori, A. Zabala, N. Otaño, W. Tato, and X. Gómez, “Development of a modular fretting wear and fretting fatigue tribometer for thin steel wires: Design concept and preliminary analysis of the effect of crossing angle on tangential force,” Metals (Basel)., vol. 9, no. 6, p. 674, Jun. 2019.

[5]	K. Feyrer, Wire ropes. Springer, 2007.

[6]	N. F. Casey and W. K. Lee, “The fatigue failure of large diameter six strand wire rope,” Int. J. Fatigue, vol. 11, no. 2, pp. 78–84, 1989.

[7]	D. Zhang, C. Feng, K. Chen, D. Wang, and X. Ni, “Effect of broken wire on bending fatigue characteristics of wire ropes,” Int. J. Fatigue, vol. 103, pp. 456–465, 2017.

[8]	R. B. Kalombo, M. S. Pestana, J. L. A. Ferreira, C. R. M. da Silva, and J. A. Araújo, “Influence of the catenary parameter (H/w) on the fatigue life of overhead conductors,” Tribol. Int., vol. 108, no. July 2016, pp. 141–149, 2017.

[9]	D. Erena, J. Vázquez Valeo, C. Navarro, and J. Domínguez, “New fatigue device for testing cables: Design and results,” Fatigue Fract. Eng. Mater. Struct., vol. 42, no. 8, pp. 1826–1837, 2019.

[10]	A. Cruzado, M. Hartelt, R. Wäsche, M. A. Urchegui, and X. Gómez, “Fretting wear of thin steel wires. Part 1: Influence of contact pressure,” Wear, vol. 268, no. 11–12, pp. 1409–1416, 2010.

[11]	Y. Shen, D. Zhang, J. Duan, and D. Wang, “Fretting wear behaviors of steel wires under friction-increasing grease conditions,” Tribol. Int., vol. 44, no. 11, pp. 1511–1517, 2011.

[12]	X. Wang, D. Wang, D. Zhang, S. Ge, and J. Alexander Araújo, “Effect of torsion angle on tension-torsion multiaxial fretting fatigue behaviors of steel wires,” Int. J. Fatigue, vol. 106, no. September 2017, pp. 159–164, 2018.

[13]	T. Guo, Z. Liu, J. Correia, and A. M. P. de Jesus, “Experimental study on fretting-fatigue of bridge cable wires,” Int. J. Fatigue, vol. 131, no. May 2019, 2020.

[14]	M. A. Garcia, L. A. Mendes Veloso, F. Comes de Castro, J. A. Araújo, J. L. A. Ferreira, and C. R. Moreira da Silva, “Experimental device for fretting fatigue tests in 6201 aluminum alloy wires from overhead conductors,” Wear, vol. 460–461, no. August, 2020.

[15]	J. A. Araújo, F. C. Castro, I. M. Matos, and R. A. Cardoso, “Life prediction in multiaxial high cycle fretting fatigue,” Int. J. Fatigue, vol. 134, no. October 2019, 2020.

[16]	P. H. C. Rocha, J. I. M. Díaz, C. R. M. Silva, J. A. Araújo, and F. C. Castro, “Fatigue of two contacting wires of the ACSR Ibis 397.5 MCM conductor: Experiments and life prediction,” Int. J. Fatigue, vol. 127, no. May, pp. 25–35, 2019.

[17]	J. Said, S. Fouvry, G. Cailletaud, C. Yang, and F. Hafid, “Shear driven crack arrest investigation under compressive state: prediction of fretting fatigue failure of aluminium strands,” Int. J. Fatigue, p. 105589, 2020.

[18]	J. Said, S. Garcin, S. Fouvry, G. Cailletaud, C. Yang, and F. Hafid, “A multi-scale strategy to predict fretting-fatigue endurance of overhead conductors,” Tribol. Int., vol. 143, no. July 2019, 2020.

[19]	A. Cruzado, S. B. Leen, M. A. Urchegui, and X. Gómez, “Finite element simulation of fretting wear and fatigue in thin steel wires,” Int. J. Fatigue, vol. 55, pp. 7–21, 2013.

[20]	S. Beretta and M. Boniardi, “Fatigue strength and surface quality of eutectoid steel wires,” Int. J. Fatigue, vol. 21, no. 4, pp. 329–335, 1999.

[21]	S. Beretta and S. Matteazzi, “Short crack propagation in eutectoid steel wires,” Int. J. Fatigue, vol. 18, no. 7, pp. 451–456, 1996.

[22]	J. Llorca and V. Sánchez‐Gálvez, “Fatigue Limit and Fatigue Life Prediction in High Strength Cold Drawn Eutectoid Steel Wires,” Fatigue Fract. Eng. Mater. Struct., vol. 12, no. 1, pp. 31–45, 1989.

[23]	A. Cruzado, M. A. Urchegui, and X. Gómez, “Finite element modeling and experimental validation of fretting wear scars in thin steel wires,” Wear, vol. 289, pp. 26–38, 2012.

[24]	A. Cruzado, M. A. Urchegui, and X. Gómez, “Finite element modeling of fretting wear scars in the thin steel wires: Application in crossed cylinder arrangements,” Wear, vol. 318, no. 1–2, pp. 98–105, 2014.

[25]	I. Llavori, A. Zabala, M. A. Urchegui, W. Tato, and X. Gómez, “A coupled crack initiation and propagation numerical procedure for combined fretting wear and fretting fatigue lifetime assessment,” Theor. Appl. Fract. Mech., vol. 101, no. September 2018, pp. 294–305, 2019.

[26]	I. R. McColl, J. Ding, and S. B. Leen, “Finite element simulation and experimental validation of fretting wear,” Wear, vol. 256, no. 11–12, pp. 1114–1127, 2004.

[27]	J. J. Madge, S. B. Leen, and P. H. Shipway, “A combined wear and crack nucleation--propagation methodology for fretting fatigue prediction,” Int. J. Fatigue, vol. 30, no. 9, pp. 1509–1528, 2008.

[28]	K. Pereira, T. Yue, and M. Abdel Wahab, “Multiscale analysis of the effect of roughness on fretting wear,” Tribol. Int., vol. 110, no. December 2016, pp. 222–231, 2017.

[29]	P. Arnaud and S. Fouvry, “A dynamical FEA fretting wear modeling taking into account the evolution of debris layer,” Wear, vol. 412–413, no. February, pp. 92–108, 2018.

[30]	L. Tang, S. Ding, Y. Xie, and Y. Huo, “A multilayer nodes update method in FEM simulation of large depth fretting wear,” Wear, vol. 301, no. 1–2, pp. 483–490, 2013.

[31]	I. Llavori, “Simulación numérica y validación experimental de fenómenos de desgaste y fatiga por fretting en aceros trefilados de reducido diámetro,” Mondragon Unibertsitatea, 2016.

[32]	N. A. Bhatti and M. Abdel Wahab, “Fretting fatigue crack nucleation: A review,” Tribol. Int., vol. 121, no. December 2017, pp. 121–138, 2018.

[33]	I. Llavori, J. A. Esnaola, A. Zabala, M. Larrañaga, and X. Gomez, “Fretting: Review on the Numerical Simulation and Modeling of Wear, Fatigue and Fracture,” in Contact and Fracture Mechanics, InTech, 2018.

[34]	S. Vantadori, G. M. J. Almeida, G. Fortese, G. C. V. Pessoa, and J. A. Araújo, “Early fretting crack orientation by using the critical plane approach,” Int. J. Fatigue, vol. 114, no. April, pp. 282–288, 2018.

[35]	C. Navarro, S. Muñoz, and J. Dominguez, “On the use of multiaxial fatigue criteria for fretting fatigue life assessment,” Int. J. Fatigue, vol. 30, no. 1, pp. 32–44, 2008.

[36]	C. Gandiolle and S. Fouvry, “Stability of critical distance approach to predict fretting fatigue cracking: A "ℓ opt -b opt " concept,” Int. J. Fatigue, vol. 82, pp. 199–210, 2016.

[37]	K. N. Smith, P. Watson, and T. H. Topper, “A Stress-Strain Function for the Fatigue of Metals,” J. Mater., vol. 5, pp. 767–778, 1970.

[38]	J. J. Madge, S. B. Leen, I. R. McColl, and P. H. Shipway, “Contact-evolution based prediction of fretting fatigue life: effect of slip amplitude,” Wear, vol. 262, no. 9, pp. 1159–1170, 2007.

[39]	M. A. Miner, “Cumulative damage in fatigue,” J. Appl. Mech., vol. 12, no. 3, pp. A159--A164, 1945.

[40]	J. J. Madge, “Numerical Modelling of the Effect of Fretting Wear on Fretting Fatigue,” The University of Nottingham, 2008.

[41]	D. Taylor, The theory of critical distances: a new perspective in fracture mechanics. Elsevier, 2010.

[42]	C. Navarro, J. Vázquez, and J. Domínguez, “Nucleation and early crack path in fretting fatigue,” Int. J. Fatigue, vol. 100, pp. 602–610, 2017.

[43]	A. Zabala, D. Infante-García, E. Giner, S. Goel, J. L. Endrino, and I. Llavori, “On the use of the theory of critical distances with mesh control for fretting fatigue lifetime assessment,” Tribol. Int., vol. 142, no. October 2019, p. 105985, 2020.

[44]	D. Infante-García, E. Giner, H. Miguélez, and M. Abdel Wahab, “Numerical analysis of the influence of micro-voids on fretting fatigue crack initiation lifetime,” Tribol. Int., vol. 135, no. January, pp. 121–129, 2019.

[45]	D. Infante-García, I. Llavori, A. Zabala, and E. Giner, “The minimum shear stress range criterion and its application to crack orientation prediction in incomplete contact fretting problems,” Int. J. Fatigue, p. 105223, Aug. 2019.

[46]	I. Llavori et al., “Critical analysis of the suitability of crack propagation direction criteria for 2D cylindrical plain fretting contact,” Eng. Fract. Mech., vol. 214, pp. 534–543, Apr. 2019.

[47]	S. M. O’Halloran, A. D. Connaire, A. M. Harte, and S. B. Leen, “A global-local fretting analysis methodology and design study for the pressure armour layer of dynamic flexible marine risers,” Tribol. Int., vol. 142, no. August 2019, p. 105967, 2020.

[48]	R. Hojjati-talemi, M. A. Wahab, J. De Pauw, and P. De Baets, “Tribology International Prediction of fretting fatigue crack initiation and propagation lifetime for cylindrical contact con fi guration,” Tribiology Int., vol. 76, pp. 73–91, 2014.

[49]	M. Caspers and C. Mattheck, “Weighted Averaged Stress Intensity Factors of Circular‐Fronted Cracks in Cylindrical Bars,” Fatigue Fract. Eng. Mater. Struct., vol. 9, no. 5, pp. 329–341, 1987.

[50]	I. Llavori, A. Zabala, A. Aginagalde, W. Tato, J. J. Ayerdi, and X. Gómez, “Critical analysis of coefficient of friction derivation methods for fretting under gross slip regime,” Tribol. Int., no. September, p. 105988, 2019.

[51]	M. A. Meggiolaro and J. T. P. Castro, “Statistical evaluation of strain-life fatigue crack initiation predictions,” Int. J. Fatigue, vol. 26, no. 5, pp. 463–476, 2004.

[52]	A. Cruzado, S. B. Leen, M. A. Urchegui, and X. Gómez, “Finite element simulation of fretting wear and fatigue in thin steel wires,” Int. J. Fatigue, vol. 55, pp. 7–21, 2013.

[53]	K. Lambrighs, I. Verpoest, B. Verlinden, and M. Wevers, “Influence of the load ratio on the threshold stress intensity factor range for heavily drawn steel wires,” Eng. Fail. Anal., vol. 18, no. 2, pp. 694–699, 2011.

[54]	K. Lambrighs, M. Wevers, B. Verlinden, and I. Verpoest, “A fracture mechanics approach to fatigue of heavily drawn steel wires,” Procedia Eng., vol. 10, pp. 3259–3266, 2011.

[55]	D. Infante-García, M. Marco, A. Zabala, F. Abbasi, E. Giner, and I. Llavori, “On the Role of Contact and System Stiffness in the Measurement of Principal Variables in Fretting Wear Testing,” Sensors, vol. 20, no. 15, p. 4152, Jul. 2020.

[56]	A. Cruzado, M. Hartelt, R. Wäsche, M. A. Urchegui, and X. Gómez, “Fretting wear of thin steel wires. Part 2: Influence of crossing angle,” Wear, vol. 273, no. 1, pp. 60–69, 2011.

[57]	B. González, J. C. Matos, J. Ayaso, and J. Toribio, “Análisis micro- y macroscópico de la fractura anisótropa en aceros eutéctoides progresivamente trefilados,” in Anales de la Mecánica de Fractura, 2007, vol. 1, pp. 111–116.

[58]	D. Socie and G. Marquis, Multiaxial Fatigue. SAE, 2000.